## Slide 1: Preparation of semi-conducting polymers dispersed in organic media
Dr. Abdulkarim CHARBA

## Slide 2: Introduction: semi-conducting polymers
Conjugated structure
Doping procedure

## Slide 3: Exemples of conjugated polymers

## Slide 7
PI-X: functionalized polyisoprene
Organic solvent: easy to evaporate and safe for electronic circuits

## Slide 8
Dispersion polymerization of EDOT in the presence of PI-Py as a stabilizer
Spherical particles of 25-50 nm diameter
PI-Py (62000g/mol ) (40wt %)
Spherical particles of 40-80 nm diameter
PI-Py (62000g/mol ) (20wt %)
Spherical particles of 50-80 nm diameter
PI-Py (62000g/mol ) (8 wt %)
TEM images of PEDOT particles prepared in the presence of PI-Py
run | Stabilizer | Mn(stabilier) (g/mole) | Wt% of PI-Py introduced b | T(°C) | solvent | σ (S/cm) | Particles diameter (nm) c
7 | PI-Py | 62000 | 40% | 50 | Toluene/propanol :9/1 | 0.003 | 25-50
2 | PI-Py | 62000 | 20% | 50 | Toluene/propanol :9/1 | 0.016 | 40-80
8 | PI-Py | 62000 | 8% | 50 | Toluene/propanol :9/1 | 0.1 | 50-80
b)Versus the monomer c)Calculated by TEM
Effect of the PI-Py concentration

## Slide 9
Dispersion polymerization of EDOT in the presence of PI-Py as a stabilizer
run | Stabilizer | Mn(stabilier) (g/mole) | Wt% of PI-Py introduced b | T(°C) | solvent | σ (S/cm) | Particles diameter (nm) c
7 | PI-Py | 62000 | 40% | 50 | Toluene/propanol :9/1 | 0.003 | 25-50
2 | PI-Py | 62000 | 20% | 50 | Toluene/propanol :9/1 | 0.016 | 40-80
8 | PI-Py | 62000 | 8% | 50 | Toluene/propanol :9/1 | 0.1 | 50-80
b)Versus the monomer c)Calculated by TEM
Effect of the PI-Py concentration
Increasing the concentration  more stable particles at the beginning of the reaction
 Smaller particles at the end of the reaction.

## Slide 10
18/12/2019
Dispersion polymerization of EDOT in the presence of PI-Py as a stabilizer
particles of 50-80 nm diameter
PI-Py (62000g/mol ) (50wt %)
l particles of 60-120 nm diameter
PI-Py (47000g/mol ) (50wt %)
particles of 80-150 nm diameter
PI-Py (16100g/mol ) (50wt %)
TEM images of PEDOT particles prepared in the presence of PI-Py
b)Versus the monomer
c)Calculated by TEM
Effect of the molecular weight of PI-Py
particles of 100-250nm
PI-Py (10000g/mol ) (50wt %)
Mn (ω-Py-PI) (g/mole) | wt% of ω-Py-PIa | T (°C) | Particles size (nm) b
3800 | 60% | 50 | agglomérat
10000 | 50% | 50 | 100-250
16100 | 50% | 50 | 80-150
47000 | 50% | 50 | 60-120
62000 | 50% | 50 | 50-80
The efficiency of the stabilizer increase with its molecular weight
The efficiency of the stabilizer increase with its molecular weightmore stable particles at the beginning of the reaction  Smaller particles at the end of the reaction.

## Slide 12: Preparation of polyaniline latex (PANI)

## Slide 13
Alarm, sensors, flexible interrupters

## Slide 14
Preparation of PANI dispersion
Pani latex
Conducting textiles
Alarm sensor, flexible interrupters
Doping-Dedoping of PANI
Insulating structure (EB)
Conducting structure (ES)

## Slide 15
Alarm, sensors, flexible interrupters

## Slide 18: Comparison between PEDOT and PANI particle
PEDOT particles are smaller than PANI particles

## Slide 19
Conclusion
Very small and well-defined PEDOT particles were obtained in the presence of various end capped PI used as a stabilizer in toluene.
Only 8 wt% of PI-Py (Mn=62000 g/mol) is needed to obtain very small PEDOT particles with a diameter of 80-100 nm.
Smaller particles were obtained with higher concentration or higher molecular weight of the stabilizer.
Efficiency of PI-Py is higher than the ones of PI-Fluo and PI-MeTh.
Sable particules of PANI in different solvents were obtained with two different technics.

## Slide 20: Perspectives  Applications
Alarm sensors
Textiles  flexible electrode, flexible interrupters.
Electromagnetic shielding.
Solar cells